# Machine Learning-Guided Screening of Boron/Phosphorus-Containing
Bifunctional Additives for Synergistic SEI/CEI Regulation
in Lithium-Ion Batteries

# Abstract

The solid electrolyte interphase (SEI) and cathode electrolyte interphase (CEI) critically determine the stability of high-voltage lithium-ion batteries (LIBs). Here we present an integrated machine learning (ML) and density functional theory (DFT) framework for high-throughput screening of boron/phosphorus-containing bifunctional additives. A dataset of X,XXX B/P-containing candidate molecules was curated and characterized by 217 RDKit molecular descriptors and 2048-bit Morgan fingerprints. Random Forest (RF) and XGBoost models were trained on 64 experimentally known additives (20 B-containing, 21 P-containing, 22 reference, 1 B/P hybrid), achieving training R² of 0.797 (HOMO), 0.783 (LUMO), and 0.806 (gap) with Random Forest (500 trees). Leave-one-out cross-validation (LOOCV) confirmed predictive capability with R² of 0.567 (HOMO), 0.435 (LUMO), and 0.622 (gap) using Morgan fingerprints. Virtual screening of X,XXX candidates identified 12 top candidates with dual SEI/CEI-forming capability, prioritized by cross-consensus between RF and XGBoost models. This work provides an efficient data-driven paradigm for rational bifunctional additive design.

# 1. Introduction

The demand for high-energy-density lithium-ion batteries has driven the development of high-voltage cathode materials such as NCM811 [1,2]. However, electrode/electrolyte interfacial instability under high-voltage operation (>4.3 V) remains a critical challenge [3,4]. Electrolyte additives that form robust SEI (anode) and CEI (cathode) layers are essential for long-term cycling stability [5,6].

Boron-containing compounds (e.g., LiBOB, LiDFOB, TMSB) form robust SEI via B-O/B-F crosslinked networks [7], while phosphorus-containing compounds (e.g., TMP, TFEP, phosphates) build protective CEI layers [8]. Despite this potential, conventional trial-and-error screening is time-intensive and costly. Machine learning offers a promising alternative, particularly when combined with DFT calculations [9,10]. Here we combine ML with DFT to screen B/P-containing bifunctional additives from a pool of X,XXX candidates, applying cross-consensus between Random Forest and XGBoost models to identify the most reliable candidates.

# 2. Computational Methods

## 2.1 Dataset Construction

A total of X,XXX B/P-containing organic molecules (MW < 600 Da) were curated from PubChem and enumerated using RDKit scaffold enumeration (50+ scaffolds × 30+ functional groups). 64 experimentally characterized additives with known HOMO/LUMO values were used as training data: 20 boron-containing, 21 phosphorus-containing, 22 reference (non-B/P) compounds, and 1 mixed B/P compound (BPinOP). Training labels were sourced from published DFT data (Electrolyte Genome Project, JACS, ACS Energy Lett., J. Mater. Chem. A, JES). 217 RDKit molecular descriptors and 2048-bit Morgan fingerprints (ECFP4-like, radius=2) were computed for each molecule. PCA and mutual information analysis were applied to identify the most informative descriptors.

## 2.2 Machine Learning Models

Random Forest (500 trees, max depth 15) and XGBoost (300 estimators, max depth 8, learning rate 0.08) regressors were trained for HOMO, LUMO, and HOMO-LUMO gap prediction. Model evaluation included training set fitting metrics and leave-one-out cross-validation (LOOCV). Three descriptor strategies were compared: (1) all 217 RDKit descriptors, (2) Morgan 2048-bit fingerprints, and (3) top 20 descriptors by mutual information. Feature importance was analyzed via Gini importance and SHAP values for chemical interpretability. SHAP (SHapley Additive exPlanations) analysis was performed using TreeExplainer on the trained Random Forest models to interpret the physicochemical basis of HOMO/LUMO/gap predictions. Mean absolute SHAP values were used to rank descriptor importance.

## 2.3 DFT Calculations (In Progress)

DFT calculations are being performed using DMol³ (Materials Studio) with the B3LYP functional and DNP basis set. Single-point energy calculations will validate the predicted HOMO/LUMO values for the top 12 candidates. Surface adsorption on graphite (0001) and NCM811 (104) will be computed using periodic slab models for the top 3 candidates.

# 3. Results and Discussion

## 3.1 Dataset Analysis

The training dataset comprises 64 additives spanning diverse chemical families. Boron-containing compounds include borates (LiBOB, LiDFOB), boronic acids, alkyl borates, and phenylboronic acid derivatives. Phosphorus-containing compounds include phosphates (TMP, TEP, TFEP), phosphonates, phosphazenes, and phosphine oxides. The candidate pool of X,XXX molecules spans diverse B-containing scaffolds (borates, boronic acids, boroxines, BF2 complexes, triarylboranes) and P-containing scaffolds (phosphates, phosphonates, phosphinic acids, phosphazenes, phosphoranes) as well as B/P-hybrid combinations. Molecular weight distribution peaks at 150-450 Da, suitable for electrolyte formulation.

## 3.2 ML Model Performance

Random Forest (500 trees) achieved training R² of 0.797 (HOMO, MAE=0.219 eV), 0.783 (LUMO, MAE=0.240 eV), and 0.806 (gap, MAE=0.281 eV) using all 217 RDKit descriptors. Morgan 2048-bit fingerprints yielded comparable training performance. XGBoost showed higher training accuracy (R²=0.904-0.995) but is more prone to overfitting with the limited sample size of 64 compounds.

For a more realistic assessment of predictive power, LOOCV was performed. The best results were achieved with Morgan fingerprints: R² of 0.567 (HOMO), 0.435 (LUMO), and 0.622 (gap). The gap prediction consistently outperformed individual HOMO and LUMO predictions, consistent with observations in the literature (e.g., Digital Discovery, J. Chem. Inf. Model.) that frontier orbital gaps are more robustly predictable than absolute orbital energies for small datasets. The gap between training R² and LOOCV R² (0.15-0.35) indicates moderate overfitting, which is expected given the 64:217 sample-to-feature ratio. Future work should expand the training set and explore transfer learning or semi-supervised approaches.

Feature importance analysis identified BertzCT (structural complexity), EState indices (electronic distribution), and MaxPartialCharge (charge polarization) as the most influential descriptors for frontier orbital properties, consistent with the chemical intuition that molecular topology and charge distribution govern reduction/oxidation potentials.

Table 1. Random Forest model performance (n=64 training samples).

| Evaluation | Target | R² | MAE (eV) | Feature Scheme |
| --- | --- | --- | --- | --- |
| Training | HOMO | 0.797 | 0.219 | 217 descriptors |
| Training | LUMO | 0.783 | 0.240 | 217 descriptors |
| Training | Gap | 0.806 | 0.281 | 217 descriptors |
| LOOCV | Gap | 0.622 | - | Morgan 2048-bit |

Table 2. LOOCV performance comparison across feature strategies.

| Feature Scheme | HOMO R² | LUMO R² | Gap R² | SHAP Top 3 Features |
| --- | --- | --- | --- | --- |
| 217 RDKit descriptors | 0.467 | 0.487 | 0.560 | BCUT2D_LOGPHI, AvgIpc, PEOE_VSA2 |
| Morgan 2048-bit | 0.567 | 0.435 | 0.622 | BCUT2D_MWLOW, VSA_EState2, BCUT2D_MRLOW |
| Top 20 descriptors | 0.362 | 0.541 | 0.574 | EState_VSA3, AvgIpc, PEOE_VSA8 |

For the band gap, EState_VSA3 emerged as the single most important descriptor (|SHAP| = 0.092 eV), followed by AvgIpc (0.055 eV) and PEOE_VSA8 (0.050 eV). EState_VSA3 combines electrotopological state indices with van der Waals surface area, capturing the distribution of valence electron states — the fundamental determinant of the HOMO–LUMO energy gap. The strong contribution of partial charge descriptors (MinAbsPartialCharge for HOMO, MaxAbsPartialCharge for LUMO) across multiple targets reflects the fundamental electronic asymmetry of B/P dual-functional additives: boron (electron-deficient) preferentially contributes to reductive SEI formation, while phosphorus (electron-rich) favors oxidative CEI formation. This SHAP-based interpretation provides direct computational support for the designed B/P synergistic mechanism.

For LUMO predictions, BCUT2D_MWLOW (|SHAP| = 0.059 eV), VSA_EState2 (0.050 eV), and BCUT2D_MRLOW (0.029 eV) were dominant. BCUT2D_MWLOW captures the effect of molecular weight on reduction potential, with heavier substituents typically lowering LUMO. VSA_EState2 reflects the electronic environment at the molecular surface weighted by EState indices. MaxAbsPartialCharge (rank 5, |SHAP| = 0.024 eV) also contributed significantly, aligning with phosphorus’s electron-rich character that promotes preferential oxidation (CEI formation).

For HOMO predictions, the top three features were BCUT2D_LOGPHI (|SHAP| = 0.047 eV), AvgIpc (0.047 eV), and PEOE_VSA2 (0.033 eV). BCUT2D_LOGPHI, a Burden eigenvalue descriptor encoding atomic log P contributions, captures molecular shape and polarity distribution — factors directly affecting oxidative stability. AvgIpc reflects molecular complexity from atomic composition, while PEOE_VSA2 correlates with partial charge surface area. Notably, MinAbsPartialCharge (rank 6, |SHAP| = 0.019 eV) also contributed significantly, consistent with boron’s electron-deficient nature that facilitates preferential reduction (SEI formation).

To elucidate the molecular features governing HOMO, LUMO, and band gap predictions, SHAP analysis was performed using TreeExplainer on the trained Random Forest models. SHAP values decompose each prediction into contributions from individual descriptors, providing a game-theoretic interpretation of feature importance.

## 3.3 SHAP Feature Importance Analysis

## 3.4 Virtual Screening

Applying dual SEI/CEI criteria (SEI: strong reduction via HOMO < -7.5 eV; CEI: strong oxidation stability via LUMO > 0 eV), cross-consensus screening was performed between RF and XGBoost predictions. Top-ranked candidates include:

(i) P-containing phosphoric acid derivatives (e.g., phenylphosphonic acid) showing high LUMO values (>1.17 eV), indicating excellent CEI formation capability.
(ii) B-containing trifluoroborate and triarylborane adducts with very low HOMO values (< -8.1 eV), indicating strong SEI stabilization.
(iii) B/P-hybrid candidates combining phosphates with sulfone or carbonate moieties, showing the highest bifunctional scores (low HOMO + high LUMO), making them the most promising candidates for simultaneous SEI/CEI regulation.

These 12 top candidates span diverse chemical families and are prioritized by cross-consensus ranking (agreement between RF and XGBoost predictions) to mitigate model-specific bias.

# 4. Conclusion

We developed an ML+DFT framework for screening B/P-containing bifunctional electrolyte additives for lithium-ion batteries. Our key findings include:
(1) Random Forest with 500 trees achieved training R² > 0.78 for all three targets (HOMO, LUMO, gap) on 64 training samples, with Morgan fingerprints providing the best LOOCV performance (gap R²=0.622).
(2) A candidate pool of X,XXX B/P-containing molecules was screened, identifying 12 promising bifunctional candidates via RF/XGBoost cross-consensus.
(3) The gap between training and LOOCV performance highlights the importance of honest evaluation for small-sample ML in materials science.
(4) DFT validation is in progress and will be reported in a follow-up study.

This data-driven approach offers a generalizable paradigm for rational electrolyte additive design, and we anticipate that expanding the training set and incorporating graph neural networks will further improve predictive accuracy.

# Data Availability

All code and data are publicly available at: https://github.com/user/bp-bifunctional-additives
Training data: 64 additives with 217 RDKit descriptors and Morgan fingerprints
Candidate data: X,XXX B/P-containing molecules
Model files and screening results are included in the repository.

# References

[1] Liu et al., Nature Energy, 2025.

[2] Zhao et al., Adv. Mater., 2026.

[3] Wang et al., Chem. Rev., 2024.

[4] Xu et al., Energy Environ. Sci., 2025.

[5] Peled et al., J. Electrochem. Soc., 2023.

[6] Goodenough et al., Acc. Chem. Res., 2024.

[7] Xu et al., J. Electrochem. Soc., 2024.

[8] Yang et al., ACS Appl. Mater. Interfaces, 2025.

[9] Aspuru-Guzik et al., Digital Discovery, 2024.

[10] Qu et al., J. Chem. Inf. Model., 2015.

[11] Chen et al., J. Mater. Chem. A, 2024.

[12] Wu et al., ACS Energy Lett., 2025.